Technical Data Sheet

Technical Data Sheet

Ref: NRPA10000

Issued: 02.10.20

Number of pages: 2

Rockfon Acoustic Glue

CHARACTERISTICS

- Solvent–free dispersion formula

- Interior use

- No need to support with mechanical fixings

- 250 kg/m2 initial tack*

- Fast drying on absorbent surfaces

- High adhesion

- Over paintable once dry

- Gap filling up to 10 mm.

- Minimum application temperature +10°C

- Low odour

* Henkel internal laboratory method: 25 g/cm²

APPLICATION FIELD

Rockfon Acoustic Glue is suitable for the following interior surfaces: plaster, concrete, cellular concrete, pumice, fiber concrete, plaster board, gypsum boards, wood materials (e.g. chip boards) and polyurethane rigid-foams.

Not recommended for constant water immersion or areas of permanent damp.

INSTRUCTIONS FOR USE

Pretreatment

Ensure surfaces to be bonded are clean and free of dust, grease or oil. Surfaces should not be continuously damp. The substrate must have a temperature of at least +10 °C.

The product dries by water evaporation, so one surface must be porous to ensure a solid, secure bond.

On very adsorbent substrates such as gypsum, chipboard (not OSB), clay-brick, the glue can dry too quickly around the outer perimeter of the application, preventing the inside of the bonded area from fully drying. To prevent this, moisten very absorbent surfaces with water from a spray bottle before applying the adhesive.

Application

Apply with a coarse-toothed/broad-toothed spatula (4–8 mm spacing and depth).
Areas of 10–15 x 10–15 cm.
• Board size 600 x 600 mm = 4 spots
• Board size 600 x 1200 mm = 6 spots
Depending on the thickness of the board and the evenness/flatness of the substrate, bead gluing can be used. The board must be fixed immediately, but no later than 10 minutes after application with a slight twisting action to ensure good contact. It does not need support while drying. Final strength is achieved after 1–2 days.

Remove any excess from the surface immediately with a damp sponge.

When bonding onto uneven surfaces or when fixing very heavy items, additional fixings or support may be required

TECHNICAL DATA

| Composition | Dispersion |
| --- | --- |
| Density | approx. 1,30 g/cm3 |
| Heat resistance | -20°C up to +70°C |
| Open time | approx. 15 min |
| Application temperature | +10°C up to +40°C |
| Initial tack | 24 - 28 g/cm3 |
| Final strength (DIN EN 205) | 5 to 6 N/mm² |
| Shelf Life | 18 months |
| Drying time | 24 h |

LIMITATIONS

Cleaning

Immediately remove any adhesive residue with a damp cloth. Cured material can only be removed mechanically.

Storage

Store cool, dry and unopened, up to 18 months.

Store away from heat, flame, and spark in a cool area. Because the product contains water, it is best stored above freezing.

Once opened, be sure to close the lid. Use the entire bucket shortly after opening.

HEALTH AND SAFETY

Before using the product please see related Material Safety Data Sheet which is available on request.

The information provided in this Technical Data Sheet (TDS) including the recommendations for use and applications of the product are based on our knowledge and experience of the product as at the date of this TDS. The product can have a variety of different applications as well as differing application and working conditions in your environment that are beyond our control. Henkel is, therefore, not liable for the suitability of our product for the production processes and conditions in respect of which you use them, as well as the intended applications and results. We strongly recommend that you carry out your own prior trials to confirm such suitability of our product.

Any liability in respect of the information in the Technical Data Sheet or any other written or oral recommendation(s) regarding the concerned product is excluded, except if otherwise explicitly agreed and except in relation to death or personal injury caused by our negligence and any liability under any applicable mandatory product liability law.

Henkel Norden AB

Box 1155

SE-172 23 Sundbyberg

Sweden